SS323-002020-01	September 9, 2020

VIRGINIA DEPARTMENT OF TRANSPORTATION

2020 ROAD AND BRIDGE SUPPLEMENTAL SPECIFICATIONSSQ315-000120-00

SECTION 323 – ASPHALT PATCHING OF EXISTING FLEXIBLE AND RIGID  PAVEMENT AND SHOULDERS

SECTION 323 – ASPHALT PATCHING OF EXISTING FLEXIBLE AND RIGID  PAVEMENT AND SHOULDERS of the Specifications is inserted as follows:

## 323.01 – Description

This work shall consist of repairing specified sections of existing flexible, rigid or composite pavements by removing all or part of the defective materials in the sections and replacing them with asphaltmix paving material. The locations of the repairs will be specified in the Contract or directed by the Engineer.

Partial Depth Hydraulic Cement Concrete (HCC) Patching shall consist of the removal of areas of unsound HCC pavement material to a depth of no more than 50 percent of the maximum pavement thickness and replacement with asphalt concrete as specified in the Contract document and as directed by the Engineer.  The pavement thickness is defined as the thickness of the HCC.

Shoulder Patching shall consist of the removal of specified areas of the full thickness of the pavement section in the shoulder only to the top of the base material (bound or un-bound) and replacement with asphalt concrete as specified in the Contract or as directed by the Engineer.

323.02 – Materials

- Asphalt concrete mixtures shall conform to Section 211.

- Tack coat shall conform to Section 310.

323.03 – Equipment

Saw cutting equipment shall be capable of sawing neat vertical faces along the patch boundaries. The use of a carbide-toothed wheel saw shall not be permitted for sawing the patch boundaries in rigid pavements.  A carbide-tipped wheel saw may be used for additional saw cuts provided that a minimum 3-inch clearance from the sawed boundary is maintained.

Material in the areas identified for shoulder patching may be removed by a milling machine, backhoe, or other excavating equipment as approved by the Department.

Equipment for furnishing and placing asphalt concrete overlay shall conform to Section 315.

323.04 – Procedures

Asphalt patches shall be placed in accordance with Section 315.  The existing pavement shall be removed with a minimum disturbance to the aggregate base material and the faces of the remaining pavement shall be cut to a smooth, vertical face without ragged edges.

The existing pavement shall be removed by milling, grinding, saw cutting or any other approved method to the specified depth for the full perimeter of the designated area. The Contractor shall clean this area of any debris or lose particles before applying tack. Tack coat shall be applied to surface and vertical faces of exposed asphalt concrete at a rate of 0.2 gallon per square yard. Exposed base aggregate shall be primed with tack coat at an application rate of 0.4 gallon per square yard. Where HCC is encountered on bitumen over concrete composite pavements before reaching the specified depth, the depth of the patch shall then be limited to the top elevation of the HCC.  Before applying the patch, the bottom of the excavation of all patches shall be cleaned of all loose and foreign materials and stabilized by hand or mechanical tamping.

HCC pavement to be removed shall be sawed along the transverse and longitudinal boundaries, including the lane and shoulder/lane joints as shown on the Plans or as directed by the Engineer. Additional saw cuts inside the patch boundaries will be permitted to facilitate the concrete removal operation. During the removal operations, utmost care shall be exercised to minimize disturbance and damage to the reinforcing steel, and the adjacent pavement and shoulder. Before applying the patch, the bottom of the excavation of all patches shall be cleaned of all loose and foreign materials.

Manual placement will be permitted for installation of the asphalt concrete, when approved by the Engineer. Control strip and pavement profile measurements will not be required. Density shall conform to Section 315.05(e). Variation between surfaces at the run on and run off joints shall not be more than 1/4 inch when tested with a 10-foot straight edge. When the surface of the asphalt patch will also be the final riding surface, that surface shall conform to the tolerances in Section 315.07(a). The Contractor shall correct humps and depressions exceeding the specified tolerance or the defective work shall be removed and replaced with new material.

The existing pavement materials that are removed shall be hauled away from the repair site immediately, and disposed of properly by the Contractor in accordance with Section 106.04.

Minimum and maximum lift thickness for patching with Superpave asphalt concrete mixes shall be maintained during construction of the patches in conformance with the following:

| SUPERPAVE ASPHALT CONCRETE LIFT THICKNESS (PATCHING) |  |  |  |
| --- | --- | --- | --- |
| NMAS (mm) | MINIMUM (in) | MAXIMUM (in) | RECOMMENDED (in) |
| 9.0 | 0.75 | 1.5 | 1.0 |
| 9.5 | 1.25 | 2.0 | 1.5 |
| 12.5 | 1.5 | 2.0 | 1.75 |
| 19.0 | 2.0 | 3.0 | 2.0 |
| 25.0 | 2.5 | 4.0 | 3.0 |

Patching and surface preparation shall be completed before the overlay or resurfacing. If an Asphalt Patch fails before overlay, the Contractor will be responsible for removing and replacing the failed patch at no cost to the Department.

323.05 – Measurement and Payment

Payment for all patching will be adjusted for density in accordance with Section 315.05(e) and Table III-6.

Partial Depth HCC Patching will be measured in square yards and will be paid for at the Contract square yard price for the mix and depth specified. This price shall be full compensation for furnishing materials and installing pavement patches complete in place. The work shall include, but not be limited to supplying materials, saw cutting, milling, grinding, removing and disposing of existing material, the cost to haul and place asphalt concrete, and all labor, equipment, tools, supervision, fuel and incidentals necessary to complete the work.

Shoulder Patching will be measured in square yards and will be paid for at the Contract square yard price for the mix and depth specified. The payment shall be full compensation for furnishing materials and installing pavement patches on the shoulder complete in place. The work shall include, but not be limited to supplying materials, saw cutting, milling, grinding, removing and disposing of existing material, the cost to haul and place asphalt concrete, and all labor, equipment, tools, supervision, fuel and incidentals necessary to complete the work.

Travel Lane Patching will be measured in tons and will be paid for at the Contract ton price for the mix specified. The payment shall be full compensation for furnishing materials and installing pavement patches in the travel lanes complete in place. The work shall include, but not be limited to supplying materials, saw cutting, milling, grinding, removing and disposing of existing material, the cost to haul and place asphalt concrete, and all labor, equipment, tools, supervision, fuel and incidentals necessary to complete the work.Liquid asphalt tack or prime will not be measured for separate payment and the cost to furnish and apply the liquid asphalt shall be included in the bid price for patching.

When Surface Preparation and Restoration is a Pay Item, that Pay Item will include the work designated in the corresponding Pay Item Definition below and be paid at the Contract price. Otherwise, that work shall meet the descriptions herein and will be measured and paid for as described herein.

Surface Preparation and Restoration Type I is a localized disintegration of the pavement, including distorted areas, no more than 5 inches in depth and no more than 20 square feet in surface area. Surface Preparation and Restoration Type I will be measured in tons of asphalt material and paid for at the rate of three times the Contract ton price of the mix types of asphalt authorized by the Engineer. This price shall include removing and disposing of unsuitable material, preparing the area, furnishing and applying tack coat, furnishing and applying asphalt material, and compaction.

Surface Preparation and Restoration Type II is a localized disintegration of the pavement, including distorted areas, no more than 5 inches in depth and more than 20 square feet in surface area. Surface Preparation and Restoration Type II will be measured in tons of asphalt material and paid for at the rate of four times the Contract ton price of the mix types of asphalt authorized by the Engineer. This price shall include removing and disposing of unsuitable material, preparing the area, furnishing and applying tack coat, furnishing and applying asphalt material, and compaction.

Surface Preparation and Restoration Type III is a localized disintegration of the pavement more than 5 inches in depth with limits of the surface area as defined by the Engineer. Surface Preparation and Restoration Type III will be measured in tons of asphalt material and paid for at the rate of five times the Contract ton price of the mix types of asphalt authorized by the Engineer. This price shall include removing and disposing of unsuitable material, preparing the area, furnishing and applying tack coat, furnishing and applying asphalt material, and compaction.

Payment will be made under:

| Pay Item | Pay Unit |
| --- | --- |
| Partial Depth PCC Patching (Asphalt Patch Mix Type and Depth) | Square Yard |
| Shoulder Patching (Shoulder Mix Type and Depth) | Square Yard |
| Travel Lane Patching (Patch Mix Type) | Ton |
| Surface Preparation and Restoration (Type) | Ton |