SS405-002020-01	June 23, 2020

VIRGINIA DEPARTMENT OF TRANSPORTATION

2020 ROAD AND BRIDGE SUPPLEMENTAL SPECIFICATIONS

SECTION 405 – PRESTRESSED CONCRETE

SECTION 405 – PRESTRESSED CONCRETE  is amended as follows:

Section 405.02(i) – Fully or partially embedded steel attachments to the prestressed concrete members is renamed to Fully or partially embedded steel attachments and replaced with the following:

Fully or partially embedded steel attachments to the prestressed concrete members shall be stainless steel when using stainless-steel or carbon-fiber-reinforced-polymer strands. When using carbon-steel strands, these same steel attachments shall be galvanized in accordance with Section 233.