SS412-002020-02	April 6, 2021

VIRGINIA DEPARTMENT OF TRANSPORTATION

2020 ROAD AND BRIDGE SUPPLEMENTAL SPECIFICATIONS

SECTION 412 – WIDENING, REPAIRING, AND RECONSTRUCTING EXISTING STRUCTURES

SECTION 412 – WIDENING, REPAIRING, AND RECONSTRUCTING EXISTING STRUCTURES of the Specifications is amended as follows:

Section 412.03(b)6 – Concrete superstructure surface repair is amended by replacing the second paragraph with the following:

The Contractor shall place 2 x 2-W1.4 x W1.4 welded wire fabric over the entire patch area where 2 inches or more of existing concrete is removed. The welded wire fabric shall be tied to reinforcing steel where possible. If reinforcing steel is not exposed or if the steel has a spacing greater than 18 inches, the welded wire fabric shall be anchored to expansion bolts at least 3/8 inch in diameter, which the Contractor shall place along the edges of the patch. The expansion bolts shall be spaced not more than 18 inches apart and shall be embedded at least 2 inches into the concrete. The minimum thickness of repair material over reinforcing steel, including expansion bolts and welded wire fabrics, shall be 2 inches unless otherwise specified.

Section 412.03(g)6a – Preconstruction testing is amended by replacing the second and third paragraphs with the following:

Test panels shall be 24 inches by 24 inches by 6 inches deep. Using the mix design specified, each crew shall gun a set of two test panels for each gunning orientation to be encountered on the project: one test panel shall contain steel reinforcement representative of that to be used on the project; the other test panel shall be used for compressive strength verification and shall not contain any steel reinforcement. Test panels shall be finished to smooth and even surface.

For shotcrete jobs of less than 200 square feet, the Contractor shall cut the test panels containing the reinforcement with a trowel or a metal template before the initial set in the presence of the Engineer to check visually for possible voids under the reinforcement. For Shotcrete jobs of more than 200 square feet, the Contractor shall cut cores from the test panels after the concrete has hardened for at least 3 days to verify good encasement of reinforcing bars. Cores shall be cut through the steel.

On all jobs, the test panels without steel reinforcement shall be used to determine the compressive strength of the applied shotcrete. The test panels shall be cured in the field in the same manner as the structure, until the cores are cut but for a minimum of 3 days. The Contractor shall cut three cores in the presence of the Engineer no earlier than 3 days and no later than 7 days after panel preparation. Cores shall be 4 inches in diameter. After the cores are drilled, the Contractor shall wipe off the surface drill water and allow the remaining surface moisture to evaporate. When the surface appears dry, but not later than 1 hour after drilling, the Contractor shall place the cores in separate plastic bags or nonabsorbent containers and seal them to prevent moisture loss. The cores will be tested by the Department at the specified age in accordance with ASTM C42.