GUIDELINES – Use with asphalt plant mix in Bristol, Salem, and Staunton districts. {2007-c211hg0}

cn211-DB0100-00	POLISHING AGGREGATE IN ASPHALT CONCRETE - Section 211—Asphalt Concrete of the Specifications is amended as follows:

Section 211.02—Materials is amended by replacing (e) with the following:

Fine or coarse aggregate that tend to polish under traffic will not be permitted in any final surface exposed to traffic except as permitted within the limits of Section 211.04(a) and (b) of the Specifications and as designated by the Engineer or as permitted elsewhere in these Specifications.

Section 211.04—Asphalt Concrete Mixtures is amended by replacing (a) and (b) with the following:

Asphalt concrete mixtures shall conform to Table II-14 and the following:

(a)	Types SM-9.0A, SM-9.0D, SM-9.0E, SM-9.5A, SM-9.5D and SM-9.5E asphalt concrete shall consist of crushed stone, crushed slag, or crushed gravel and fine aggregate, slag or stone screenings or a combination thereof combined with asphalt cement.

NOTE:  For all surface mixes, except where otherwise noted, no more than 5 percent of all aggregate retained on the No. 4 sieve and no more than 20 percent of the total aggregate may be polish susceptible.  At the discretion of the Engineer, a SM-9.5AL may be specified and polish susceptible aggregates may be used (without percentage limits).

(b)	Types SM-12.5A, SM-12.5D, SM-12.5E, IM-19.0A, IM-19.0D, and IM-19.0E asphalt concrete shall consist of crushed stone, crushed slag, or crushed gravel and fine aggregate, slag or stone screenings or a combination thereof combined with asphalt cement.

NOTE:  At the discretion of the Engineer, an intermediate mix may be designated as either a SM-19.0A or SM-19.0D.  For SM-12.5 and SM-19.0 surface mixes, no more than 5 percent of the aggregate retained on the No. 4 sieve may be polish susceptible.  All material passing the No. 4 sieve may be polish susceptible.  No more than 35 percent of the total aggregate composition (polish and non-polish susceptible) shall be passing the No. 8 sieve.  At the discretion of the Engineer, a SM-12.5AL may be specified and polish susceptible aggregates may be used (without percentage limits).

10-7-09; Reissued 7-12-16 (SPCN)