TABLE II-14 of the Specifications is replaced with the following:

| TABLE II-14 Mix Design Criteria |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Mix Type | VTM (%) Production | VFA (%) Design | VFA (%) Production | Min. VMA (%) | Fines/Asphalt Ratio | No. of Gyrations N Design |
| SM-9.0A 1,2 | 2.0-5.0 | 75-80 | 70-85 | 17.0 | 0.6-1.3 | 50 |
| SM-9.0D 1,2 | 2.0-5.0 | 75-80 | 70-85 | 17.0 | 0.6-1.3 | 50 |
| SM-9.0E 1,2 | 2.0-5.0 | 75-80 | 70-85 | 17.0 | 0.6-1.3 | 50 |
| SM-9.5A 1,2 | 2.0-5.0 | 75-80 | 70-85 | 16.0 | 0.7-1.3 | 50 |
| SM-9.5D 1,2 | 2.0-5.0 | 75-80 | 70-85 | 16.0 | 0.7-1.3 | 50 |
| SM-9.5E 1,2 | 2.0-5.0 | 75-80 | 70-85 | 16.0 | 0.7-1.3 | 50 |
| SM-12.5A 1,2 | 2.0-5.0 | 73-79 | 68-84 | 15.0 | 0.7-1.3 | 50 |
| SM-12.5D 1,2 | 2.0-5.0 | 73-79 | 68-84 | 15.0 | 0.7-1.3 | 50 |
| SM-12.5E 1,2 | 2.0-5.0 | 73-79 | 68-84 | 15.0 | 0.7-1.3 | 50 |
| IM-19.0A 1,2 | 2.0-5.0 | 69-76 | 64-83 | 14.0 | 0.6-1.3 | 50 |
| IM-19.0D 1,2 | 2.0-5.0 | 69-76 | 64-83 | 14.0 | 0.6-1.3 | 50 |
| IM-19.0E 1,2 | 2.0-5.0 | 69-76 | 64-83 | 14.0 | 0.6-1.3 | 50 |
| BM-25.0A 2,3 | 1.0-4.0 | 67-87 | 67-92 | 13.0 | 0.6-1.3 | 50 |
| BM-25.0D 2,3 | 1.0-4.0 | 67-87 | 67-92 | 13.0 | 0.6-1.3 | 50 |
| 1Asphalt content should be selected at 4.0% air voids for A & D mixes, 3.5% air voids for E mix. 2Fines-asphalt ratio is based on effective asphalt content. 3Base mix shall be designed at 2.5% air voids. BM-25A shall have a minimum asphalt content of 4.4% unless otherwise approved by the Engineer. BM-25D shall have a minimum asphalt content of 4.6% unless otherwise approved by the Engineer. |  |  |  |  |  |  |

6-4-20 (SPCN)