cq211-000310-00 [formerly cq211-030100-00]

GUIDELINES – For asphalt maintenance projects in Bristol district coal counties only when called for by the District Maintenance Engineer. {2007-cu211000a}

SM-22.5 ASPHALT CONCRETE MIXTURES (Bristol District Coal Counties Only) — When asphalt concrete mix types SM-22.5 A, D, or E are specified in the Schedules, TABLE II-13—Asphalt Concrete Mixtures: Design Range of the Specifications shall be amended to add the following to the table:

TABLE II-13

Asphalt Concrete Mixtures: Design Range1

| Mix Type | Percentage by Weight Passing Square Mesh Sieves |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 2 in | 1 ½ in | 1 in | ¾ in | ½ in | 3/8 in | No. 4 | No. 8 | No. 30 | No. 50 | No. 200 |
| SM-22.5 A,D,E |  |  | 95-100 | Max. 90 | 60-84 |  |  | 19-38 |  |  | 2-8 |

10-21-08; Reissued 7-12-16_(SPCN)