cq302-DB0100-00

GUIDELINES: For use with SP302-DB0300-01.

cq302-DB0100-00

GRAB STRENGTH FOR PREFABRICATED VERTICAL DRAINS – The geotextile jacket material for Prefabricated Vertical Drains shall conform to Section III-1F of the Special Provision for Prefabricated Vertical Drains, except that Grab Tensile Strength shall be at least 120 lbs when tested in accordance with ASTM D4632.

9-20-17 (SPCN)