cq312-000100-00

GUIDELINES – Use when requested by the Designer.  Include SP314-000100-00, SP312-000100-00, SP512-000120-02, and SP704-000100-02.{2007-cu312001a}

CAPE SEAL TREATMENT — This work shall consist of furnishing and applying asphalt surface treatment to the existing roadway surface, allowing sufficient time for curing followed by cleanup, then furnishing and applying emulsified asphalt slurry seal as the finished surface.  The sequence of work shall be as follows:

1.	The existing asphalt surface shall be patched at locations according to the provisions of this contract and as directed by the Engineer.

2.	All pavement markings shall be eradicated according to the special provision for SECTION 512—MAINTAINING TRAFFIC (ASPHALT SCHEDULES).

3.	Asphalt surface treatment shall be applied according to the special provision for ASPHALT SURFACE TREATMENT.  Asphalt surface treatment shall be a modified single seal or modified double seal with liquid asphalt material of CRS-2L emulsified asphalt, aggregate size No. 8P, and blot coat of No. 9 aggregate.

4.	Temporary pavement markings shall be installed and maintained according to the special provision for SECTION 704—PAVEMENT MARKINGS AND MARKERS.

5.	Asphalt surface treatment shall be allowed to cure for two weeks after application.

6.	After curing, excess and loose material resulting from the vehicular traffic that occurred during the asphalt surface treatment curing period shall be removed from the roadway.

7.	Emulsified asphalt slurry seal shall be applied according to the special provision for EMULSIFIED ASPHALT SLURRY SEAL.  Emulsified asphalt slurry seal shall be Type B or C applied at a rate of 20 pounds per square yard.

8.	Temporary and permanent pavement markings shall be installed according to the special provision for SECTION 704—PAVEMENT MARKINGS AND MARKERS.

Cape seal treatment will be measured and paid for according to the appropriate asphalt surface treatment and emulsified asphalt slurry seal pay items and pay units specified in the Contract to complete the work.

10-21-14; Reissued 7-12-16_(SPCN)