GUIDELINES – For use in NOVA District only, unless approved by the State Specifications Engineer.

LATEX-MODIFIED SLURRY SEAL

The SPECIAL PROVISION FOR EMULSIFIED ASPHALT SLURRY SEAL is amended as follows:

Section II-A – Asphalt Emulsion is replaced with the following:

Asphalt Emulsion:  Emulsified asphalt shall conform to Section 210 of the Specifications; except it shall be a quick setting emulsion and the following requirements shall apply:

1.	The emulsion shall be designated CQS-1h or CQS-1hLM cationic quick setting emulsion and shall conform to Cationic Type CSS-1h. CQS-1hLM shall additionally conform to the following:

- Ring and ball softening point of the residue shall be at least 140°F.

- Pass towel test (VTM-89) in 30 minutes at room temperature with job materials.

- Residue, percent by evaporation, minimum 62% as determined by VTM-78.

- Material shall be furnished in accordance with the Virginia Asphalt Acceptance Program.

2.	The Cement Mixing Test will not be enforced.

3.	Emulsion Setting Time - Prior to shipment of each new formulation of emulsified asphalt, the Contractor shall perform a towel test to verify that the emulsion will set quickly enough to accommodate early release of traffic. Testing for setting time shall be according to VTM-89.

8-27-19 (SPCN)