cq317-DB0100-00

SECTION 317—STONE MATRIX ASPHALT CONCRETE PLACEMENT of the Specifications is amended as follows:

317.08—Compaction is amended to replace the second paragraph with the flowing:

The Design-Builder shall approach the use of vibratory rollers on SMA with caution to minimize coarse aggregate fracture/breakage in the aggregate skeleton of SMA mixes. If the Design-Builder elects to use a vibratory roller, the mat should receive not more than three vibratory passes. The Design-Builder shall use the roller only on the highest frequency and lowest amplitude setting.

1-10-19 (SPCN)